Plastics – A General Review:

Plastics are man-made materials. Plastics have taken the place of traditional materials like woods and metals.

Plastics differ from other materials largely because of the size of their molecules. Most materials have molecules made up of less than 300 atoms, plastics contain thousands of atoms. We call them Macromolecules.

Some plastics are derived from natural substances such as animals, insects and plants but most are man-made. These are named Synthetic Plastics.

Most synthetic plastics come from crude oil but coal and natural gas is also used.
When crude oil is refined gasses are given off. The gasses are broken down into Monomers. These are chemical substances consisting of a single molecule. Thousands of these are linked together in a process called Polymerization to form new compounds called Polymers.

By the application of heat and pressure to the plastic granules, we can get the required shape. Several processes like injection molding, extrusion, compression molding, transfer molding etc. are used to make the plastic products.

Plastic Products

Scientists who discovered the plastic materials:

| Material | Year | Discovered By |
| --- | --- | --- |
| NATURAL RUBBER | 1839 | GOODYEAR |
| VULCANITE | 1843 | HANCOCK |
| GUTTA-PERCHA | 1843 | MONTGOMERIE |
| SHELLAC | 1856 | CRITCHLOW |
| BOIS DURCI | 1856 | LEPAGE |
| PARKESINE | 1862 | PARKES |
| XYLONITE | 1869 | SPILL |
| CELLULOID | 1870 | HYATT |
| CELLULOID PHOTOGRAPHIC FILM | 1889 | GOODWIN |
| VISCOSE | 1892 | CROSS, BEVAN & BEADLE |
| CELLULOSE ACETATE | 1894 | CROSS & BEVAN |
| CASEIN | 1903 | KUNTH |
| BAKELITE | 1907 | BAEKELAND |
| DAMARD LACQUER | 1910 | SWINBURNE |
| POLYVINYL ACETATE | 1913 | KLATTE |
| UREA FORMALDEHYDE | 1918 | JOHN |
| POLYACRYLATES | 1927 | ROHM & HAAS |
| BEETLE THIOUREA | 1928 | ROSSITER |
| POLYSTYRENE | 1929 | IG FARBEN |
| NEOPRENE | 1930 | CAROTHERS |
| POLYESTERS & POLYAMIDES | 1930 | CAROTHERS |
| POLYMETHYL METHACRYLATE | 1932 | CRAWFORD - I C I |
| MELAMINE | 1933 | HENKEL |
| POLYVINYLCHLORIDE | 1933 | SEMON - B. F. GOODRICH |
| POLYESTER RESIN | 1933 | CARLTON ELLIS |
| POLYETHYLENE (LOW DENSITY) | 1933 | GIBSON & FAWCETT- ICI |
| POLYVINYLIDENE CHLORIDE | 1933 | WILEY - DOW |
| NYLON 66 | 1935 | HILL - DU PONT |
| NYLON 6 | 1938 | SCHLACK |
| PTFE | 1938 | PLUNKETT- DU PONT |
| POLYURETHANE | 1939 | BAYER - IG FARBEN |
| EPOXIDE RESIN | 1939 | CASTAN |
| POLYACRYLONITRILE | 1940 | DU PONT |
| POLY(ETHYLENE TEREPHTHALATE) | 1941 | WHINFIELD AND DICKSON |
| SILICONES | 1943 | KIPPING |
| POLYETHYLENE (HIGH DENSITY) | 1953 | ZIEGLER |
| POLYPROPYLENE | 1954 | NATTA |
| POLYCARBONATE | 1958 | FOX |
| POLYFORMALDEHYDE | 1959 | McDonald |
| ETHYLENE VINYL ACETATE (EVA) | 1960 | DU PONT |
| POLYIMIDE | 1962 | DU PONT |
| POLYPHENYLENE OXIDE (PPO) | 1964 | GENERAL ELECTRIC |
| POLYSULPHONE | 1965 | UNION CARBIDE |

List of Acronyms for plastics:

| ABS AI BOPP BOPS CA CAB CAP CF CFRP CN COPE CP CPE CPVC CS CTA CTFE DMC EAA EC ECTFE EP EPS ETFE ETP EVA FEP FR FRP GP GRP HDPE HIPS HMWPE LCP LDPE LLDPE MC MDPE MF OPP OPS PA PAI PAN PAS PBI PBMA PBT PC PE PEEK PEI PES PET PETG PF PHB PHV PI PMMA PMP POM PP PPE PPMI PPO PPS PPSU PPT PS PSF PSO PTFE PTMT PU PVAc PVAl PVB PVC PVCA PVDC PVDF PVF PVF2 PVFM PVK PVOH PVT SAN SHIPS SMC TPX UF UHMWPE uPVC VC/E VC/MA VC/VDC XLPE XPS | Acrylonitrile-butadiene-styrene copolymer Amide-imide copolymer Biaxially oriented PP (film) Biaxially oriented PS (film) Cellulose acetate Cellulose acetate butyrate Cellulose acetate proprionate Cresol formaldehyde Carbon fibre reinforced plastics Cellulose nitrate Copolyester-ether Cellulose proprionate Chlorinated PE Chlorinated PVC Casein Cellulose triacetate Chloro-trifluoroethylene Dough moulding compound Ethylene-acrylic acid copolymer Ethyl cellulose Ethylene-chl;orotrifluoroethylene Epoxide resin Expanded PS Ethylene-tetrafluorethylene copolymer Engineering thermoplastics Ethylene vinyl acetate copolymer Perfluoro (ethylene-propylene) copolymer Flame retardant polymer Fibre reinforced plastics General purpose grade of plastic Glass (fibre) reinforced polyester High density PE High impact polystyrene High molecular weight PE Liquid crystal polymer Low density PE Linear LDPE Methyl cellulose Medium density PE Melamine formaldehyde Oriented PP (film) Oriented PS (film) Polyamide (Nylon) Poly amide-imide Polyacrylonitrile Polyaryl sulphone Polybenzimidazole Polybutyl methacrylate Polybutylene terephthalate Polycarbonate Polyethylene Poly ether-ether-ketone Poly ether-imide Polyethersulphone Polyethylene terephthalate Glycol modified PET Phenol formaldehyde Polyhydroxybutyrate Polyhydroxyvalerate Polyimide Polymethyl methacrlyate Poly-4-methyl pentene-1 Polyoxymethylene (Acetal) Polypropylene Polyphenylene ether Polypyromellitimide Polyphenylene oxide Polyphenylene sulphide Polyphenylene sulphone Polypropylene terephthalate Polystyrene Polysulphone Polysulphone Polytetrafluoroethylene Polytetramethylene terephthalate (PBT) Polyurethane Polyvinyl acetate (Poly(vinyl ethanoate)) Polyvinyl alcohol Polyvinyl butyral Polyvinyl chloride Polyvinyl chloride-acetate copolymer Polyvinylidene chloride Polyvinylidene fluoride Polyvinyl fluoride Polyvinylidene fluoride Polyvinyl formal Polyvinyl carbazole Polyvinyl alcohol Polyvinyl toluene Styrene-acrylonitrile copolymer Super HIPS Sheet moulding compound Poly-4-methyl pentene-1 Urea formaldehyde Ultra high molecular weight PE Unplasticised PVC Vinyl chloride-ethylene copolymer Vinyl chloride-methyl acrylate copolymer Vinyl chloride-vinylidene chloride copolymer Crosslinked PE Expanded PS |
| --- | --- |

Classification of Plastics:

According to Chemical Nature:

- Organic Plastics

- Inorganic Plastics

Organic Plastics:

Organic compounds contain carbon and carbon-hydrogen bonds. Organic compounds don't contain metal atoms.

Inorganic Plastics:

Inorganic compounds don’t contain carbon and carbon-hydrogen bonds. Organic compounds contain metal atoms. It can be used as semiconductors.

According to Thermal Behavior:

- Thermoplastics and

- Thermoset Plastics

Thermoplastics are made up of lines of molecules with few cross linkages. This allows them to soften when heated and to be bent into a variety of shapes and forms. They become stiff and solid again when cold. This process can be repeated many times

Thermosetting Plastics are made up of lines of molecules which are heavily cross linked. It creates a rigid molecular structure. They may be heated the first time and shaped but they become permanently stiff and solid. They cannot be reshaped again

Plastic Memory Each time a plastic is reheated it will attempt to return to its original flat shape unless it has been over heated or damaged. This is called a plastic memory

Thermoplastics:

- PE,

- PP, PVC,

- Nylon,

- POM etc.,

Thermosets:

- Phenol Formaldehyde,

- Urea Formaldehyde,

- Melamine Formaldehyde,

- Unsaturated Polyester Resin

- Poly Bismaleimides etc.,

General Classification of Plastics:

- Commodity Plastics

- Engineering Plastics

- Specialty Plastics

Commodity Plastics:

- Polyethylene,

- Polypropylene,

- Polyvinylchloride,

- Polystyrene

Engineering Plastics:

- Nylon,

- Polyacetals,

- Polycarbonate,

- PEEK (Poly Ether Ether Ketone)

- Polyester Resin,

- PBT (Poly Butylene Terephthalate) etc.,

Specialty Plastics:

- Ply Sulphones,

- Poly imides,

- Polyphenylene Oxide

- Poly Sulphoxy Methylene etc.,

| Plastics Chooser Chart |  |  |  |  |
| --- | --- | --- | --- | --- |
| Common Name | Properties | Uses | Common Forms | Cost |
| Rigid PVC (poly vinyl chloride) | Wide range of colors. Stiff, hard. Tough at room temperature. Can be used outdoors if suitably stabilized. Light weight. Very good acid and alkali resistance. Particularly good for fabricating. Thermoplastic | Pipes, guttering and fittings. Bottles and containers. Curtain rails. Roofing sheets. Shoe soles. Brush bristles. | Powders. Pastes. Liquids. Sheets. Wide range of colors. | Medium |
| Polystyrene (high impact polystyrene) | Not tough. Comes in a wide range of colors. Thermoplastic | Good for vacuum forming. Join using a liquid polystyrene cement. | Shell forms for containers, model boats and model cars. | Low |
| ABS (acrylonitrile butadiene styrene) | Stiff, strong and tough. Scratches easily. Comes in a wide range of colors. Thermoplastic. | Frameworks and mechanical parts, links, cams and wheels | Easy to cut and trim using liquid solvent cement. | Medium |
| Nylon ( Polyamide) | Hard, tough, rigid, creep resistant. Good bearing surface. Self-lubricating. Resistant to oil, fuels and chemicals. High melting point. Very resilient. Wear and friction resistant. Thermoplastic | Gear wheels, bearings, automotive, agricultural, general communications and telecommunications equipment parts. Power tool casings. Curtain rail fittings, packaging, film, clothing, combs. | Powder, granules, chips, rods, tubes, sheet, extruded sections. Usually white or cream. Other colors including black obtainable. | High |
| Polyester resin (Unsaturated polyester resin) | Good electrical insulator, good heat resistance. Stiff, hard, brittle alone but strong and resilient when laminated. Resistant to ultraviolet light for outside use. Strongly exothermic, this can lead to cracking. Contracts on curing. Thermosetting Plastic | GRP boats, car bodies. Chair shells. Ducting, garden furniture, etc. Translucent panels for building. Encapsulating and embedding castings. | Liquids. Pastes. | Medium |
| Low density polythene (Low density polyethylene) | Wide range of colors. Tough. Good chemical resistance. Good electrical insulator. Flexible, soft. Fades unless light stabilized. Attracts dust unless anti-static. | Squeeze bottles and toys. Plastic sacks and sheets. Packaging film. Telecommunications cable insulation. TV aerial lead insulation. | Powders. Granules. Films. Sheets. Wide range of colors. | Medium |
| High density polystyrene ( High density polyethylene) | Wide range of colors. Fairly stiff and hard. Stiffness and softening point both increase with density. Can be sterilized. Good chemical resistance. High impact resistant. Fades unless light stabilized. | Milk crates. Bottles, barrels, tanks, pipes, chemical pumps, machine parts (e.g. gear wheels). House ware( e.g. buckets, bowls) | Powders, granules, films. Sheets. Wide range of colors. | Medium |
| Plasticized PVC (polyvinyl chloride) | Wide range of colors. Soft, flexible. Good electrical insulator. | Leather cloth, suitcases, and tabletops coverings. Sealing compounds, under seal. Dip coatings. Hosepipes. Electrical wiring insulation. Wall coverings( vinyl wallpapers). Floor coverings. | Powders, pastes. Liquids. Sheets. Wide range of colors. | Medium |
| Expanded polystyrene (Expanded polyphenyl ethane) | Very buoyant. Light weight. Absorbs shocks. Very good sound and heat resistor. Crumbles easily. Burns readily unless flame proofed. | Sound insulation. Heat resistant packaging. | Sheets, slabs, beads. Usually white. | Low |
| Acrylic ( Polymethyl methacrylate) | Stiff, hard glass clear. Very durable outdoors. Easily machined, cemented and polished. Good electrical insulator. Safe with food. Ten times more impact resistance than glass.. Splinters easily. Scratches easily. | Light units and illuminated signs. Watch and clock glasses. Record player lids. Simple lenses. Aircraft canopies and windows. Car rear light units. Skylights. Furniture. Baths. Perspex sheet. Cladding for buildings. | Rods, tubes which are usually clear. Translucent and opaque. Comes in a wide range of colors. | Medium |

Details of different plastics normally we use in our life:

Polyethylene:

Ethylene monomer is polymerized to form Polyethylene. The techniques used for polymerizing the ethylene are low pressure process, High pressure process and metallocene catalyzed process. There are three major types of polyethylene.

Types:

HDPE (High Density Poly Ethylene)

LDPE (Low Density Poly Ethylene)

HDPE:

A linear polymer, High Density Polyethylene (HDPE) is prepared from ethylene by a catalytic process. It is having more closely packed structure with a higher density and somewhat higher chemical resistance than LDPE. HDPE is also somewhat harder and more opaque and it can withstand rather higher temperatures (120° C for short periods, 110° Celsius continuously). High density polyethylene lends itself particularly well to blow molding,

Pipes

Properties:

- Good chemical resistance.

- Good low temperature toughness (to -60'C),

- Flexible,

- Translucent / waxy,

- Weatherproof,

- Tensile Strength: 4550 psi

- Specific Gravity: 0.95

Thermal Properties:

- Maximum Temperature: 248°F 120°C

- Minimum Temperature: -148°F -100°C

- Melting Point: 266°F 130°C

Special Characteristics:

- Easy to process by most methods,

- Weldable and machinable

Applications:

- Good choice for trays and tanks

- Irrigation pipes,

- Pipe fittings,

- Wear plates,

- Cutting boards

- Cable insulation,

- Carrier bags,

- Food wrapping.

LDPE (Low Density Poly Ethylene):

Low Density Polyethylene (LDPE) was originally prepared some fifty years ago by the high pressure polymerization of ethylene. Its comparatively low density arises from the presence of a small amount of branching in the chain (on about 2% of the carbon atoms). This gives a more open structure. Low Density Polyethylene (LDPE) is a most useful and widely used plastic especially in dispensing bottles or wash bottles.

Connectors

Properties:

- Good chemical resistance,

- Semi-rigid,

- Translucent,

- Very tough,

- Tensile Strength: 1700 psi,

- Weatherproof,

- Low water absorption,

- Specific Gravity: 0.92

Thermal Properties:

- Maximum Temperature: 176°F 80°C

- Minimum Temperature: -58°F -50°C

- Melting Point: 248°F 120°C

Special Characteristics:

LDPE can be processed by most methods.

Applications:

- Squeeze bottles,

- Toys,

- Carrier bags,

- High frequency insulation,

- Chemical tank linings,

- Heavy duty sacks,

- General packaging,

- Gas and water pipes.

Polypropylene:

Propylene monomer is polymerized to form polypropylene. Polypropylene is one of those rather versatile polymers out there. It serves double duty, both as a plastic and as a fiber. As a plastic it's used to make things like dishwasher-safe food containers. It can do this because it doesn't melt below 160oC, or 320oF.

Lid of a Tic-tac

Properties:

- Semi-rigid,

- Translucent,

- Good chemical resistance,

- Tough,

- Good fatigue resistance,

- Integral hinge property,

- Tensile Strength: 4,500 psi,

- Good heat resistance,

- Specific Gravity: 0.90

Thermal Properties:

Maximum Temperature: 275°F 135°C

Minimum Temperature: 32°F 0°C

Melting Point: 338°F 170°C

Special Characteristics:

Great chemical resistance makes Polypropylene a popular choice for plating and chemical tanks, as well as laboratory cabinetry and semi-conductor bench tops. PP can be mechanically joined with screws or rivets.

Applications:

- Flexible and rigid packaging,

- Automotive Bumpers, cladding, and exterior trim,

- Consumer products like bottle caps, chairs and buckets

- PP files and ropes

- PP fiber is used in tape and strapping.

Polyvinyl chloride (PVC):

Polyvinyl chloride (PVC) is a major thermoplastic material finding use in a very wide variety of applications and products. Poly (vinyl chloride) is the plastic known at the hardware store as PVC. It is manufactured from a monomer called vinyl chloride.  PVC is mostly used in electrical applications because of its excellent electrical insulation and self extinguishing characteristics. PVC can be made much useful by the addition of ingredients. PVC's major benefit is its compatibility with many different kinds of additives, making it a highly versatile polymer. PVC can be plasticized to make it flexible for use in flooring and medical products.

Reducer Bushing

Bathtub Test Apparatus

Properties:

- PVC has excellent electrical insulation properties,

- Good impact strength and weatherproof

- Tensile Strength: 6,500 psi

- Good UV resistance

- Specific Gravity: 1.34

- Clear and rigid,

- Resistance to dilute and concentrated acids,

Thermal Properties:

Maximum Temperature: 158°F 70°C

Minimum Temperature: -13°F -25°C

Melting Point: 176°F 80°C

Special Characteristics:

Compatibility with many different kinds of additives - PVC can be clear or colored, rigid or flexible, formulation of the compounding is the key to PVC's "added value".

Applications:

- Popular material for tanks and fittings,

- Commonly used for nuts, bolts, ducts, hoods, and process tanks

- Window frames,

- Drainage pipe,

- Water service pipe,

- Medical devices,

- Blood storage bags,

- Cable and wire insulation,

- Resilient flooring,

- Roofing membranes,

- Automotive interiors and seat coverings,

- Fashion and footwear,

- Packaging,

- Cling film,

- Credit cards,

- Synthetic leather and other coated fabrics.

Polystyrene:

Polystyrene is a polymer made from the monomer styrene, a liquid hydrocarbon. At room temperature, polystyrene is normally a solid thermoplastic, but can be melted at higher temperature for molding or extrusion, then resolidified. Styrene is an aromatic monomer, and polystyrene is an aromatic polymer.

Spoon

CD Case

Properties:

- Excellent X-ray resistance,

- Transparent,

- Low shrinkage,

- Brittle,

- Rigid,

- Tensile Strength: 2600-10200 psi

- Free from odor and taste,

- Heat resistance is low,

- Specific Gravity: 1.05

Thermal Properties:

Maximum Temperature: 93°C

Melting point: 190°C

Special Characteristics:

Highly transparent cases made from crystal polystyrene. High transparency, low cost and easy mouldability have established its supremacy in presentation packing.

Applications:

- Toys and novelties,

- Rigid packaging,

- Refrigerator trays and boxes,

- Cosmetic packs and costume jewels,

- Lighting diffusers,

- Audio cassette and CD cases.

Acrylonitrile Butadiene Styrene:

ABS is a copolymer made by polymerizing styrene and acrylonitrile in the presence of polybutadiene. The proportions can vary from 15% to 35% acrylonitrile, 5% to 30% butadiene and 40% to 60% styrene. Ease of processing has led ABS becoming the most popular of the engineering polymers.

Panel

Properties:

- The nitrile groups from neighboring chains, being polar, attract each other and bind the chains together, making ABS stronger than pure polystyrene.

- The styrene gives the plastic a shiny, impervious surface.

- The butadiene, a rubbery substance, provides resilience even at low temperatures.

- ABS material combines the strength and rigidity of the acrylonitrile and styrene polymers with the toughness of the polybutadiene rubber.

- Stability under load is excellent with limited loads.

- ABS has good electrical properties that are fairly constant over a wide range of frequencies.

- ABS polymers are resistant to aqueous acids, alkalis, concentrated hydrochloric and phosphoric acids, alcohols and animal, vegetable and mineral oils, but they are swollen by glacial acetic acid, carbon tetrachloride and aromatic hydrocarbons and are attacked by concentrated sulfuric and nitric acids.

- Tensile Strength: 4,300 psi

- Specific Gravity: 1.04

Thermal Properties:

ABS can be used between −25 °C and 80 °C.

Melting Point: 221°F 105°C

Special Characteristics:

It can be thermo-formed, pressure formed, blow molded, sheared, sawed, drilled, or even "cold stamped".

Joints can be ultrasonic welded, thermo-welded, and chemically bonded.

Applications:

- Commonly used for telephone bodies,

- Safety helmets,

- Piping,

- Furniture,

- Car components,

- TV casings,

- Radios,

- Control panels,

- Valve bodies, and

- Material handling equipment.

Polyamide (Nylon):

Nylon (Polyamide), invented in 1928 by Wallace Carothers (DuPont) is considered to be the first engineering thermoplastic. Nylons are typified by amide groups (CONH) and encompass a range of material types (e.g. Nylon 6,6; Nylon 6,12; Nylon 4,6; Nylon 6; Nylon 12 etc.), providing an extremely broad range of available properties. The majority of nylons tends to be semi-crystalline and is generally very tough materials with good thermal and chemical resistance.

Grills

Bearings

Properties:

- The majority of nylons tends to be semi-crystalline and is generally very tough with good thermal and chemical resistance.

- Impact resistant material

- Tensile Strength: 5,800 psi

- Specific Gravity: 1.13

- Nylons tend to absorb moisture from their surroundings

- Poor dimensional stability

Thermal Properties:

Maximum Temperature: 210°F 99°C

Minimum Temperature: -94°F -70°C

Melting Point: 420°F 216°C

Special Characteristics:

Nylon’s very low coefficient of friction and abrasion resistant makes it to use as gears and bearing.

Applications:

- Nylon is commonly used in the production of tire cords, rope, belts, filter cloths, sports equipment and bristles.

- Door Handles & Radiator Grills

- Ski Bindings & In-line Skates

- Nylon fibers are used in textiles, fishing line and carpets.

- Nylon films is used for food packaging, offering toughness and low gas permeability, and coupled with its temperature resistance, for boil-in-the-bag food packaging.

- Low Voltage Switch Gears:

- This has a range of sub-category applications, miniature circuit breakers, residual current devices, fuses, switches and relays, contactors and cabinets.

Polyacetals (POM):

Acetal is a popular and versatile crystalline engineering polymer. Acetal became commercially available in 1960. Acetal is a popular and versatile crystalline engineering polymer.

Ball cage

Properties:

- Polyacetal is an opaque, very hard, and highly crystalline polymer that offers excellent strength and stiffness in many applications like automotive or sporting goods.

- Tensile Strength: 8,800 psi

- Specific Gravity: 1.41

Thermal Properties:

Maximum Temperature: 180°F 80°C

Minimum Temperature: -40°F -40°C

Melting Point: 320°F 160°C

Special Characteristics:

Acetal is a tough material with good dimensional stability, and a low coefficient of friction. Acetal machines well and is relatively easy to process.

Applications:

- Transportation - fuel pumps and other fuel system components, control cables, windshield wipers, heater/air conditioner control system components, interior door handles, and seat belt components

- Industrial products - faucet underbodies, shower heads, pumps, irrigation equipment and valves, conveyor links

- Appliance components - gears, timers and pumps

- Information technology products - gears and bearings

- Consumer products - gears, springs, hand tools, toys

Polycarbonates (PC):

Polycarbonates are a particular group of thermoplastic polyesters. They are easily worked, molded, and thermoformed; as such, these plastics are very widely used in modern manufacturing. Their interesting features (temperature resistance, impact resistance and optical properties) position them between commodity plastics and engineering plastics. In recent years Polycarbonate blends have become increasingly commercially important. PC is widely used in blends due to its excellent compatibility with a range of polymers. ABS/PC is one among that which shows excellent properties under all circumstances.

Glasses

Properties:

- Polycarbonates are strong, stiff, hard, tough, transparent engineering thermoplastics

- Very good dimensional stability

- Tensile strength: 70-80 N/mm2

- Excellent flame resistant with self extinguishing nature

- Specific Gravity: 1.2

- Poor weathering in an UV light environment

Thermal Properties:

Maximum Service Temperature: 135°C

Minimum Service Temperature: -100 °C

Melting Point: 149 °C

Special Characteristics:

- Polycarbonate is one of the toughest transparent sheets available, about 300 times stronger than single-strength glass.

- Can be joined mechanically, solvent bonded, and welded with lots of practice

Applications:

Electrical & Electronics (E&E):

- Power distribution (covers and housings)

- Connectors

- Electrical household appliances

- Mobile phones

- Electrical chargers

- Lighting

- Battery boxes

Automotive

- Automotive lighting

- Head lamp lenses

- Dashboards

- Interior cladding

- Exterior parts (bumpers, body panels)

General Industries / Packaging

- Power tools

- Baby bottles

- Water dispensers

- Garden equipment

- Furniture (office & institutional)

- Sporting goods

- Medical applications

Polyurethanes:

Polyurethane is a unique material that offers the elasticity of rubber combined with the toughness and durability of metal. Because urethane is available in a very broad hardness range (eraser-soft to bowling-ball-hard), it allows the engineer to replace rubber, plastic and metal with the ultimate in abrasion resistance and physical properties. The sales and production of Polyurethane increasing every year. Polyurethane can be produced in a wide range of hardness.

PU products

Properties:

- Urethanes have better abrasion and tear resistance than rubbers, while offering higher load bearing capacity.

- Compared to plastics, urethanes offer superior impact resistance, while offering excellent wear properties and elastic memory.

- Polyurethane has excellent resistance to oils, solvents, fats, greases and gasoline.

- Polyurethane has a higher load-bearing capacity than any conventional rubber.

- Tear resistant,

- Polyurethane has outstanding resistance to oxygen, ozone, sunlight and general weather conditions.

- Excellent noise abatement properties.

- Polyurethane has excellent electrical insulating properties

- Tensile Strength: 5000 psi

- Specific Gravity:  1.12 – 1.24

Thermal Properties:

Maximum Service Temperature: 108°C

Minimum Temperature:  -60°C

Melting Temperature: 151°C

Special Characteristics:

With benefits such as weight reduction, noise abatement and wear improvements, Urethanes have replaced metals in sleeve bearings, wear plates, sprockets, rollers and various other parts.

Applications:

- Belts

- Metal forming pads

- Wear strips

- Bumpers

- Gears

- Bellows

- Machinery mounts

- Cutting Surfaces

- Sound-dampening pads

- Chute and hopper liners

- Prototype machined parts

- Gaskets

- Seals

- Rollers

- Roller covers

- Sandblast curtains and

- Diaphragms

PBT (Poly Butylene Terephthalate):

Polybutylene Terephthalate (PBT) is a crystalline, high molecular weight polymer that has an excellent balance of properties and processing characteristics. Because the material crystallizes rapidly, mold cycles are short and molding temperatures can be lower than for many engineering plastics.

High Speed Connector

Properties:

- This thermoplastic polyester has very good dimensional stability.

- It also exhibits high heat resistance, chemical resistance and good electrical resistance.

- In general, PBT materials exhibit higher tensile, flexural and dielectric strengths.

- PBT has faster and more economical molding characteristics than many thermosets.

- Compared to non-reinforced resin, glass-reinforced PBT exhibits a two-to threefold increase in tensile, flexural and compressive strengths and moduli.

- The reinforced resins exhibit good resistance to oxidation in hot air, comparable to that of nylon 6 or nylon 6/6. Water absorption values are relatively low (0.1% fro over 24 hours).

- Specific gravity: 1.31

Thermal Properties:

Maximum Service Temperature: 300 °F (149 °C)

Minimum Service Temperature:

Melting Temperature:

Special Characteristics:

PBT has very low water absorption (0.1%) and excellent mechanical properties.

Applications:

- The main applications in which the polybutylene terephthalate (PBT) is used are tightly-toleranced technical parts that are required to withstand high mechanical, electrical and thermal loading.

- PBT is used as an insulator in the electrical and electronics industries.

- PBT is used for automotive components (including “under-bonnet”) and power tool casings.

- Polybutylene terephthalate is used for door and window hardware, automobile luggage racks and body panels, headlight reflectors, and fiber optic cables.

- It is being used to replace PVC for cable sheathing, due to a combination of environmental pressures and outstanding electrical properties across a wide range of temperatures.

- PBT is also replacing metals (in conjunction with PC as an alloy/blend) for automotive body panels.

Polyester Resin:

Ethylene glycols are used as a reactant in the manufacture of polyester resins. This resin is used for making almost all commercial glass fiber reinforced plastic composites.

Yarns

Properties:

- Polyester composites are rigid, clear, chemical resistant, high strength, low creep, good electrical properties, low temperature impact resistance.

- The mechanical properties are substantially influenced by the selection of monomeric diols or dibasic acids (building blocks of polyester), their amounts and temperature of processing.

- Good Thermal conductivity

- Specific Gravity: 1.45

Thermal Properties:

Maximum Service Temperature: 300 OF (148 °C) (Aromatic Polyester)

Minimum Service Temperature: -40 °F (4.4 °C)

Melting Temperature: 500 °F (260 °C)

Special Characteristics:

Polyester resins are commonly used in elevated temperature applications, especially in the electrical and corrosion resistance areas.

Excellent resistance to radiation.

Applications:

- In light industry and chemical industry

  - Used as lubricant-free bearings, piston rings, pads, sealing packing etc. working at high temperature, or under water / or in moisture and vapor.

  - Compounded with PTFE powder to make bridge slides.

- In electronics, electric equipment and instruments industries

Heat-resistant plugs, sockets, spools, motor parts, printed circuit boards, due to its excellent thermal conductivity as well as insulation properties, the parts of Aromatic Polyester powder is able to efficiently remove the heat generated in  electronics operation so that avoid damages from part overheat.

- Blends of Aromatic Polyester Powder could be sprayed and form wearable coat on moving parts, which can dramatically elongate the coated parts' life and improve the working efficiency. Besides, Aromatic Polyester could be used in lubricant-free coating, anti-corrosion coating and anti-stick coating.

- The uses for polyester resins are extremely varied, and include boat and marine, construction materials, automotive and aircraft bodies, luggage, furnishings, appliances, textiles and packaging.

- Polyester fibers are commonly found in textile applications including clothing and carpets. Polyester films are frequently used in packaging and wraps for consumer goods, as well as video, audio and computer tapes.

Polyimide:

Polyimide (sometimes abbreviated PI) is a polymer of Imide monomers. Polyimides are a very interesting group of incredibly strong and astoundingly heat and chemical resistant polymers. Their strength and heat and chemical resistance are so great that these materials often replace glass and metals, such as steel, in many demanding industrial applications. Polyimides are even used in many everyday applications.

Aircraft Engine Cooling Tube

Properties:

- Compared to most other organic or polymeric materials, polyimides exhibit an exceptional combination of thermal stability (>500°C), mechanical toughness and chemical resistance.

- In addition, they have excellent dielectric properties.

- Specific Gravity: 1.42

- Tensile strength is 75-90 MPa

Thermal Properties:

Maximum Service Temperature: Up to 500 °C

Minimum Service Temperature: -10 °C

Melting Temperature: Won’t melt decomposes at 520 °C

Special Characteristics:

Polyimide has exceptional thermal stability of over 500 °C with good mechanical properties.

Applications:

Because of their high degree of ductility and inherently low Carbon To Ether (CTE), polyimides can be readily implemented into a variety of microelectronic applications.

- Multilayer thin and thick film applications on large silicon or ceramic substrates can be readily achieved.

- Polyimide films are frequently used as a "stress buffer" or protective overcoat for semiconductors. Polyimide stress buffers are typically 4-6 microns in thickness, and protect the delicate thin films of metal and oxides on the chip surface from damage during handling and from induced stress after encapsulation in plastic molding compound.

- Polyimides are used as Photosensitive Materials

- Polyimides are used in High-Performance Electronics Packaging and Optoelectronic Applications

Polysulphone:

Polysulphone is an amorphous and clear high-performance plastic with a light-brownish transparency. In chemistry, polysulphone (also spelled polysulfone) is abbreviated PSU. Polyethersulphone (PES), another sulphur-containing polymer, also belongs to the group of polysulphone plastics.

Pump Head

Laboratory Tubing Connectors

Properties:

- High degree of rigidity,

- A high long-term service temperature,

- Optimal electrical insulation properties and

- Resistance to contact with oil,

- Resistant to hydrolysis.

- Good radiation resistance

- Poor UV resistance

- Tensile strength: 70 MPa

- Specific Gravity: 1.24

Thermal Properties:

Lower Working Temperature: -50 °C

Upper Working Temperature: 150-180 °C

Melting Temperature Range: 310-390 °C

Special Characteristics:

- Good high temperature performance under continuous rating of 150°C (300°F).

- Good high frequency electrical properties.

- Good resistance to ionizing radiation.

Applications:

- Plumbing (tap cartridges, fittings, manifolds)

- Medical (sterilizing trays, suction bottles, respirators, nebulizers, humidifiers)

- Membranes (hemodialysis, water purification, gas separations)

- Food processing (filter bowls, microwave cookware, parts for milking machines)

- Electrical and electronics (bobbins, switch housings switch housings, capacitor film)

- Engineering (valve bodies, under-bonnet components, housings)

Polyphenylene Oxide:

A thermoplastic, linear, non-crystalline polyether obtained by the oxidative polycondensation. Polyphenylene oxide, also called polyphenylene ether, is usually blended with polystyrene to improve its toughness and processability.

Properties:

- Excellent electrical properties

- Unusual resistance to acids and bases

- Difficult to process (blended to ease injection molding)

- PPO is easily attacked by some hydrocarbons, although it resists many chemicals

- Polyphenylene oxide possesses excellent dimensional stability at high temperature and humidity conditions

- Low moisture absorption, and

- High mechanical and dielectric strength

- Rigid, tough and opaque

- Tensile Strength: 2.1.-2.50 N/mm2

- Specific Gravity: 1.06

Thermal Properties:

Maximum Service Temperature: 90 °C (194 °F)

Minimum Service Temperature: -29 °C (20 °F)

Melting Point:  154 °C (310 °F)

Special Characteristics:

PPO products are characterized by exceptional moisture resistance, high dimensional and thermal stabilities, good flame resistance and high electrical resistance properties.

Applications:

- Coffee pot and washing m/c parts (where high temperature and moisture are critical) Replacement for die castings

- Drink vending machines

- Microwave components

- Water pumps

- Automotive and electrical components

- Power tool housing

- Appliance casings and as foams in superior foam sandwich structures

- Frame and chassis material for large domestic appliances, e.g. Tumble driers, dishwashers and washing machine components

- Other large moldings such as pallets and automotive roofs

Plastic Products:

Gear

Plastic gear first emerged into large-scale use in the 1950s and soon became economical and functional alternatives to metal gears. Plastic gears are made of inexpensive commodity plastics for use in low power drives in products like clocks, motorized toys and lawn sprinklers.

Why Plastic Gears?

Plastic gears have greater consistency and are easily molded to various shapes. They are less expensive and are lighter in weight. Plastic gears are chemical and corrosion resistant and have quieter and smoother operation. They deflect to compensate for inaccuracies by absorbing tiny impacts of small tooth errors and gear misalignment. They offer more efficient drive geometry. Plastic gear ratios are feasible to allow for wider gears that transfer more power in single stage, thereby increasing load capacity.

The dimension and properties of plastic gears change with temperature, moisture absorption and chemical exposure. The plastic material can withstand high tangential force with acceptable tooth deflection. They have high strength to withstand shock loads during sudden stops and overloads. They are creep resistant and maintain contact ratio, tip clearance and overall gear geometry.

Gear Material:

The most common plastic materials used for making gears are

- Acetal,

- Polybutylene terephthalate (PBT),

- Nylon,

- Polyphenylene sulfide (PPS), and

- Liquid crystal polymer (LCP)

Nylon

Acetal

PBT

Acetal is the most important of all plastics. It offers long term dimensional stability and excellent lubricity. It is often used in gears for office equipment, irrigation equipment, autos, appliances, clocks and meters.

PBT produces extremely smooth surfaces in molding and is often used in housing.

Nylon offers toughness and wears well against other plastics. They are often used in worm gears and housings.

PPS offers high stiffness, dimensional stability and extended fatigue life.

LPC works well in small, precision gears under light loads, such as watch gears.

Disadvantages of Plastic Gears:

Plastic gears have some disadvantages also. They have reduced ability to operate at higher temperatures and can be affected negatively by many chemicals.

They are often used in water meters, showerheads, water sprinklers and other applications where water could erode metals.

Additives Used:

Glass fillers are used in the material composition to increase its strength and to reduce its shrinkage.

Headlight Lens:

Lighting systems are taking on an increasingly important role in automotive styling. Headlights don’t get the credit they deserve. They are the eyes of your vehicle. They allow you to see at night and be seen by other motorists. Cars were originally built with glass headlights that were easily broken. Most vehicles built since 1990 have polycarbonate lenses. This is a type of clear plastic that bounces back from considerable impact, making it an ideal choice for the front of a vehicle. The problem with polycarbonate is its tendency to yellow and cloud over time as a result of UV exposure. Fortunately, a number of products have been formulated to remove this haze and clarify damaged lenses with minimal cost and effort. In most cases, replacement can be avoided.

Material:

The headlight lens is made from polycarbonate. PC gives excellent transparency with impact resistance which helps to avoid breakage of headlight. Polycarbonate plastic is used because of its tensile strength and the ability to be manufactured to conform to the front end styling of a vehicle. Although it's a very hard plastic, it's also very porous so during manufacturing a protective silicone hard coat is applied to the headlight lens. This silicone hard coat is supposed to protect the headlight lens from intense sun, heat, road chemicals, bugs, humidity and acid rain, etc.

Properties:

Polycarbonates are strong, stiff, hard, tough, transparent engineering thermoplastics that can maintain rigidity up to 140oC and toughness down to -20°C or special grades even lower. The material is amorphous (thereby displaying excellent mechanical properties and high dimensional stability), is thermally resistant up to 135oC and rated as slow burning. Special flame retardant grades exist which pass several severe flammability tests.

Special Characteristics:

Polycarbonate head lamps are self extinguishing with excellent transparency and dimensional stability.

Panels:

Panels give the complete structure of the product. It gives aesthetic appearance to the product. It should be electrically insulated to avoid danger of getting shock. It should be easily moldable to get complicated structures.

Material:

The plastic panels for mobiles, telephones are made by using the polymer called ABS (Acrylonitrile Butadiene Styrene). ABS is considered superior for its hardness, gloss, toughness, and electrical insulation properties. However, it will be degraded when exposed to acetone.

Properties:

Even though ABS plastics are used largely for mechanical purposes, they also have good electrical properties that are fairly constant over a wide range of frequencies. These properties are little affected by temperature and atmospheric humidity in the acceptable operating range of temperatures. The final properties will be influenced to some extent by the conditions under which the material is processed to the final product; for example, molding at a high temperature improves the gloss and heat resistance of the product whereas the highest impact resistance and strength are obtained by molding at low temperature.

Special Characteristics:

ABS can be electroplated. It has glossy surface as of PP. ABS polymers are resistant to aqueous acids, alkalis, concentrated hydrochloric and phosphoric acids, alcohols and animal, vegetable and mineral oils.  It is tough in nature because of butadiene presence.

Additives in Plastics:

The following list provides a summary of the purpose of many of the common additives used in plastics.

| Additives | Function |
| --- | --- |
| Accelerator | Chemical used to increase the rate at which a curing process occurs in thermosetting resins |
| Antiblocking agent | These substance prevent plastic films from sticking together, and are used to facilitate handling |
| Antifogging agents | These improve packaging film clarity, by preventing any water from the contents of the package from condensing as droplets on the inside surface of the film |
| Antioxidant | Protects a polymer against oxidation, whether during processing or in service |
| Antistatic agent | Reduces or eliminates surface electrical charges and hence prevents dust pickup on polymer surfaces |
| Biocide | Protects a plastic article against attack by bacteria, fungi, algae etc., Types – fungicides and bactericides |
| Blowing agent | Substance added to polymer to generate gas which will have the effect of expanding or foaming the polymer. The gas can be produced chemically or by simple evaporation |
| Compatibilizer | Substance, usually polymeric, which when added to a mixture of two rather dissimilar polymers, enables them to become more intimately mixed |
| Coupling agent | Used to treat a surface so that bonding occurs between it and another kind of surface, e.g mineral and polymer |
| Curing agent | Promotes cross linking in polymers, e.g peroxides in polyesters, or amines in epoxy formulations |
| Diluents | A solvent which makes a solution more dilute; but in case of additives, any substance which reduces resin viscosity and hence makes processing easier. Frequently refers to epoxy resins. |
| Defoaming agent | Substance which removes trapped air form liquid mixes during compounding |
| Exotherm modifier | Substance which reduces the maximum temperature reached during an exothermic chemical reaction |
| Fiber | Reinforcement for polymers; improves mechanical properties. Length : Diameter ratio very high |
| Filler | Particulate additive designed to change polymer physical properties (e.g fire resistance, modulus, shock resistance) or to lower cost |
| Flame retardant | Substance added to reduce or prevent combustion |
| Foam catalyst | Used in PU foam production to control the foaming process and achieve satisfactory foam quality |
| Heat stabilizers | Prevents polymer form degrading thermally, even in absence of oxygen, during processing |
| Impact modifier | Substance added to use up the energy of crack propagation and hence increase resistance to impact |
| Light stabilizer | Chemical added to reduce or eliminate reactions caused by visible or UV light radiation which would otherwise cause polymer degradation in outdoor use. |
| Low profile additive | Substance added to thermosetting molding compounds to counteract shrinkage during cure and uneven surface finish |
| Lubricant | Prevents polymer form sticking to the mold or machinery and reduce melt viscosity, allowing the molten polymer to pass easily through intricate channels. It also reduce friction between polymer particles before they melt |
| Microspheres/ microballoons | Spherical filler particles usually hollow, used to reduce weight in a product without much adverse effect on mechanical properties |
| Nucleating agent | Substance which promotes or controls the formation of spherulites in crystalizable polymers. It leads to several small spherulites, rather than a few large ones |
| Odor modifiers | Used to mask an undesirable odor or to add a desirable one. Their value is dependant on the persistence of their action |
| Optical brightener | Special fluorescent organic substances used to correct discoloration or enhance whiteness. They absorb UV radiation and emits it as visible light |
| Peroxide | Source of free radicals, generally for cross linking thermosetting resins or polyolefins. Used in rubber industry and as polymerization initiators. |
| Plasticizer | Additive designed to space out the polymer molecules, facilitating their movement and leading to enhanced flexibility and ductility. Widely used to convert PVC from the rigid to flexible variety. |
| Processing aid | Used to counter processing problems, this varies with the polymer, but often means lowering the melt viscosity and improving melt homogeneity |
| Release agent | Substance designed to ease the parting of a plastic object from the mold; it may be an internal additive or coating |
| Slip agent | Kind of lubricant which have insufficient compatibility to remain inj the polymer; they migrate in to the surface and reducing tack |
| Smoke suppressant | Changes the nature of the polymer combustion process, if it is not possible to prevent it so as to reduce smoke formation |
| Surfactant | To reduce surface tension in liquids, for example they stabilize the cells of PU foams during the foaming process |
| Thickening agent | Viscosity increaser. In USP resins magnesium oxide is able to increase the viscosity so much that a liquid resins become a tack free solid suitable for making sheet molding compound. |

Price Chart for Various Plastics:

Commodity Plastics

KEY:

I-Annual volumes greater than 20 million pounds

II-Annual volumes of about 2 million to 5 million pounds

| Resin/Grade | I (Rs.) |  | II (Rs.) |  |
| --- | --- | --- | --- | --- |
| ABS |  |  |  |  |
| Injection Medium Impact |  | 90 - 93 |  | 94 - 95 |
| Injection High Impact |  | 95 - 96 |  | 98 - 102 |
| Injection Pipe fittings |  | 80 - 81 |  | 84 - 88 |
| Injection High heat |  | 116 - 120 |  | 125 - 130 |
| Injection Flame retardant |  | 121 - 125 |  | 130 - 145 |
| Extrusion Pipe GP |  | 92 - 94 |  | 97 - 102 |
| Extrusion Sheet GP |  | 109 - 110 |  | 112 - 114 |
| Blends PC/ABS |  | -- |  | 159 - 164 |
| Blends Nylon/ABS |  | -- |  | 164 - 174 |
| Acrylic |  |  |  |  |
| GP |  | -- |  | 106 - 111 |
| HDPE |  |  |  |  |
| Blow Molding Copolymer(HIC) |  | 67 - 69 |  | 71 - 73 |
| Blow Molding Homopolymer (Dairy) |  | 67 - 68 |  | 69 - 72 |
| Drums |  | 69 - 71 |  | 72 - 75 |
| Injection GP |  | 63 - 64 |  | 66 - 68 |
| Extrusion Film HMW |  | 72 - 74 |  | 76 - 79 |
| Extrusion Film MMW |  | 72 - 73 |  | 77 - 79 |
| Extrusion Pipe HMW |  | 77 - 79 |  | 82 - 85 |
| Extrusion Pipe MMW |  | 80 - 83 |  | 84 - 86 |
| Extrusion Sheet |  | 65 - 67 | P | 69 - 71 |
| Rotomolding Powder |  | -- |  | 78 - 81 |
| LDPE |  |  |  |  |
| Injection GP |  | -- |  | 79 - 81 |
| Injection Lid Resin |  | 77 - 80 |  | 81 - 83 |
| Extrusion Coating paper |  | 77 - 79 |  | -- |
| Extrusion Film liner |  | 72 - 74 |  | 75 - 80 |
| Extrusion Clarity film |  | 70 - 72 |  | 73 - 76 |
| LLDPE |  |  |  |  |
| Butene-1 comonomer Injection GP |  | -- |  | 63 - 67 |
| Butene-1 comonomer Extrusion liner film |  | 62 - 65 |  | 66 - 68 |
| HAO comonomer Injection GP |  | -- |  | 69 - 71 |
| HAO comonomer Lid resin |  | 74 - 77 |  | 80 - 83 |
| HAO comonomer Extrusion liner film |  | 68 - 70 |  | 72 - 75 |
| HAO comonomer Rotomolding powder |  | -- |  | 88 - 93 |
| PET |  |  |  |  |
| APET |  | 82 - 84 |  | 86 - 90 |
| Bottle resin |  | 72 - 74 |  | 75 - 77 |
| CPET |  | 79 - 81 |  | -- |
| PP |  |  |  |  |
| Homopolymer Injection GP |  | 71 - 73 |  | 74 - 77 |
| Extrusion Fiber |  | 70 - 72 |  | 73 - 75 |
| Extrusion Film |  | 72 - 75 |  | 76 - 77 |
| Extrusion Profiles |  | 74 - 77 |  | 79 - 83 |
| Extrusion Sheet |  | 73 - 76 |  | 77 - 79 |
| Random Copolymer Injection |  | 74 - 76 |  | 77 - 79 |
| Random Copolymer Film |  | 76 - 77 |  | 78 - 80 |
| Random Copolymer Blow molding |  | 76 - 77 |  | 79 - 82 |
| Impact Copolymer High Impact |  | 85 - 89 |  | 90 - 93 |
| Impact Copolymer TPO |  | 105 - 110 |  | 112 - 116 |
| PS |  |  |  |  |
| Crystal Injection GP |  | 81 - 83 |  | 85 - 89 |
| Crystal High Heat |  | 85 - 89 |  | 91 - 92 |
| High Impact Extrusion |  | 84 - 86 |  | 89 - 91 |
| High Impact Injection |  | 83 - 85 |  | 88 - 90 |
| High Heat injection |  | 91 - 96 |  | 97 - 99 |
| Flame retardant |  | 121 - 125 |  | 127 - 131 |
| EPS cups |  | 119 - 122 |  | -- |
| EPS unmodified |  | 115 - 118 |  | 114 - 123 |
| PVC |  |  |  |  |
| Suspension Resin Injection GP |  | 63 - 66 |  | 66 - 68 |
| Suspension Resin Pipe grade |  | 61 - 63 |  | 64 - 67 |
| Dispersion Resin Homopolymer GP |  | 63 - 67 |  | 69 - 73 |

HIGH-TEMPERATURE THERMOPLASTICS

KEY:

I-Annual volumes of about 200,000 pounds

II-Single, less-than-truckload purchases of 2,000-4,000 pounds

|  | Volume category |  |  |  |
| --- | --- | --- | --- | --- |
| Resin/Grade | I |  | II |  |
| Fluoropolymers |  |  |  |  |
| ECTFE |  | 1250 - 1442 |  | -- |
| PTFE |  | 670 - 765 |  | -- |
| PVDF |  | 720 - 760 |  | -- |
| Liquid Crystal Polymers |  |  |  |  |
| Injection Glass filled |  | 610 - 980 |  | -- |
| Injection Mineral filled |  | 550 - 810 |  | -- |
| Extrusion |  | 945 - 1180 |  | -- |
| Polyamide/imide |  |  |  |  |
| 30 glass |  | 1750 - 1750 |  | 1850 - 1850 |
| Polyarylate |  |  |  |  |
| Polyarylate |  | 176 - 210 |  | -- |
| Polyetherimide |  |  |  |  |
| Injection GP |  | 800 - 800 |  | 880 - 880 |
| 30 glass |  | 660 - 660 |  | 720 - 720 |
| Polyetherketone |  |  |  |  |
| PEEK |  | -- |  | 4500 - 4500 |
| Polyphenylene Sulfide |  |  |  |  |
| 35 glass 30 filler |  | 380 - 390 |  | 495 - 505 |
| 40 glass |  | 595 - 605 |  | 740 - 765 |
| Polysulfone |  |  |  |  |
| Injection GP |  | 392 - 392 |  | 455 - 455 |
| 30 glass |  | 331 - 331 |  | 439 - 439 |

Engineering Thermoplastics

I-Annual volumes greater than 1 million pounds

II-Annual volumes of 300,000-500,000 pounds

|  | Volume category |  |  |  |
| --- | --- | --- | --- | --- |
| Resin/Grade | I |  | II |  |
| Acetal |  |  |  |  |
| Homopolymer |  | 103 - 110 |  | 114 - 120 |
| 20 glass |  | -- |  | 145 - 160 |
| Copolymer |  | 105 - 115 |  | 120 - 129 |
| 25 glass |  | -- |  | 150 - 165 |
| Cellulosics |  |  |  |  |
| Acetate |  | -- |  | 178 - 178 |
| Butyrate |  | -- |  | 175 - 175 |
| Propionate |  | -- |  | 175 - 175 |
| Nylon |  |  |  |  |
| Type 6 |  | 165 - 175 |  | 178 - 182 |
| Type 6/6 |  | 172 - 180 |  | 184 - 195 |
| PC |  |  |  |  |
| Blow Molding |  | 170 - 180 |  | 201 - 211 |
| Injection GP |  | 154 - 163 |  | 158 - 183 |
| 20 glass |  | 170 - 180 |  | 201 - 217 |
| Injection Structural foam |  | 152 - 161 |  | 188 - 205 |
| Injection Flame retardant |  | 185 - 202 |  | 213 - 223 |
| Extrusion Sheet |  | 153 - 162 |  | 165 - 193 |
| Optical media |  | 136 - 145 |  | 146 - 165 |
| Polyester |  |  |  |  |
| PBT Injection |  | 100 - 105 |  | 110 - 115 |
| PBT 30 glass FR |  | 135 - 140 |  | 145 - 155 |
| PET Injection |  | 96 - 101 |  | 106 - 116 |
| PET 30 glass FR |  | 133 - 143 |  | 143 - 153 |
| Polyurethane |  |  |  |  |
| Ester type Injection |  | 169 - 186 |  | 193 - 202 |
| Ester type Extrusion |  | 196 - 218 |  | 232 - 250 |
| Ether type |  | 232 - 245 |  | 277 - 286 |
| PPO/PPE |  |  |  |  |
| Injection GP |  | 123 - 135 |  | 140 - 150 |
| Injection GP 20 glass |  | 179 - 190 |  | 216 - 235 |
| Injection Structural foam |  | 131 - 148 |  | 150 - 170 |
| Extrusion |  | 148 - 159 |  | 180 - 200 |
| SAN |  |  |  |  |
| GP |  | 109 - 117 |  | 121 - 145 |
| SMA |  |  |  |  |
| GP |  | -- |  | 137 - 141 |
| High Impact |  | 125 - 136 |  | 145 - 148 |
| Flame retardant |  | 175 - 183 |  | -- |
| TPE |  |  |  |  |
| Polyester |  | -- |  | 192 - 250 |
| Olefinic |  | 68 - 102 |  | 100 - 116 |
| Styrenic |  | 87 - 127 |  | 139 - 183 |
| UHMW-PE |  |  |  |  |
| UHMW-PE |  | 110 - 114 |  | 126 - 136 |

THERMOSETS

I-Annual volumes of 2 million to 5 million pounds

II-Annual volumes of about 200,000-500,000 pounds

|  | Volume category |  |  |  |
| --- | --- | --- | --- | --- |
| Resin/Grade | I |  | II |  |
| Epoxy |  |  |  |  |
| GP |  | 100 - 112 |  | -- |
| Compounds Coils bushings |  | 105 - 152 |  | -- |
| Compounds Resistors diodes |  | -- |  | 227 - 286 |
| Semiconductor Novolac |  | -- |  | 212 - 246 |
| Semiconductor Anhydride |  | -- |  | 214 - 297 |
| Melamine Molding Compound |  |  |  |  |
| Melamine Molding Compound |  | 95 - 99 |  | -- |
| Phenolic |  |  |  |  |
| GP |  | 75 - 85 |  | -- |
| Polyester Unsaturated |  |  |  |  |
| GP |  | 174 - 195 |  | -- |
| Isophthalic |  | 171 - 195 |  | -- |
| Specialty |  | -- |  | 230 - 265 |
| Polyurethane Isocyanates |  |  |  |  |
| polymeric MDI |  | 105 - 115 |  | -- |
| 80/20 TDI |  | 110 - 120 |  | -- |
| Urea Molding Compound |  |  |  |  |
| Black/Brown |  | -- |  | 67 - 78 |
| White/Ivory |  | -- |  | 72 - 83 |
| Vinyl Ester |  |  |  |  |
| Anti Corrosion |  | -- |  | 204 - 223 |
| Anti Heat/Corrosion |  | -- |  | 229 - 237 |

Recycled Plastics

| Resin/Grade | Clean regrind or flake |  | Pellets |  |
| --- | --- | --- | --- | --- |
| ABS |  |  |  |  |
| Mixed colors, industrial |  | 47 - 55 |  | 50 - 60 |
| POLYCARBONATE |  |  |  |  |
| Clear, industrial |  | 80 - 90 |  | -- |
| Mixed colors, industrial |  | 45 - 50 |  | 55 - 60 |
| POLYETHYLENE |  |  |  |  |
| HDPE: |  |  |  |  |
| Natural, post-consumer |  | 45 - 48 |  | 55 - 58 |
| Mixed colors, post-consumer |  | 32 - 34 |  | 42 - 44 |
| Mixed colors, industrial |  | 28 - 33 |  | 38 - 43 |
| HMW-HDPE film, post-consumer |  | -- |  | 38 - 44 |
| LLDPE stretch film |  | -- |  | 39 - 45 |
| Clear, post-consumer |  | -- |  | 51 - 55 |
| Colored, post-consumer |  | 25 - 30 |  | 35 - 40 |
| PET BOTTLES |  |  |  |  |
| Clear, post-consumer |  | 46 - 54 |  | 58 - 66 |
| Green, post-consumer |  | 38 - 42 |  | 48 - 52 |
| POLYPROPYLENE |  |  |  |  |
| Industrial |  | 29 - 33 |  | 40 - 44 |
| POLYSTYRENE |  |  |  |  |
| Industrial |  | 40 - 50 |  | 55 - 65 |
| High-heat crystal, post-consumer |  | 40 - 50 |  | 52 - 62 |
| PVC |  |  |  |  |
| Clear, industrial |  | 28 - 34 |  | -- |

Trade Names of Various Plastic Materials:

Trade Names A

| Trade Name | Material | Manufacturer |
| --- | --- | --- |
| Abalak | PF varnish | Kunstharzfabrik Dr. Fritz Pollak, Vienna, |
| Acelloid | CA, m | General Plastics Corp. London, SE13, England |
| Aceloid | CA | CIE, Petit-Colin-Oyonnithe, Paris, France |
| Acelose | CA | American Cellulose Company, Indianapolis, USA |
| Aceta | CA | CIE, Petit-Colin-Oyonnithe, Paris, France |
| Acetaloid | CA, m | Acetate Products Corp. Ltd. London, England |
| Acetoid | CA | Punfield & Barstow Ltd., London, England |
| Acetol | CA | Societe des Usines Chim. Rhone-Poulenc, Paris, France |
| Acetophane | CA film | Societe Industrielle de l'Acetophane, |
| Acetylon | CA | Dynamit A.G., vorm. Nobel, Hamburg, Germany |
| Agalyn | CN dentures | J.D. Whyte Co. Pittsburgh, PA. USA |
| Akalit | CS | Akalit Kunsthornwerke A.G. Vienna, Austria |
| Aladdinite | CS | Aladdinite Co. Inc. Orange NJ USA |
| Alberit | PF | Chem. Fab. DR. Kurt Albert, Wiesbaden, Germany |
| Albertol | PF | Rohm & Haas, Philadelphia, PA USA |
| Albolit | PF | Augsburger Kunstharz-Fabrik Augsburg, Germany |
| Alboresin | UF | Kontakt-Rommler A.G. Frankfurt, Germany |
| Alborid | CN | Kausch |
| Alcolite | CN | Ransom & Rudolph Co. Toledo, Ohio, USA |
| Aldur | UF | Aldur Corp. Brooklyn, NY, USA |
| Aldydal | PF | I.G. Farbenindustrie A.G. Frankfurt, Germany |
| Algalith | CS | de Charraud, Rueil, France |
| Alino | CN | R. Strauss & Co. Frankfurt, Germany |
| Alkalit | CS | Alkalit Kunsthornwerke, A.G. Vienna, Austria |
| Amalith | PF | Kausch |
| Amberdeen | PF | Kausch |
| Amberglow | PF | Labs. Industriels d'Asnieres, Paris, France |
| Amberit | PF | Kausch |
| Ambrasit | PF | Chem.Fab.Ambrasit, Vienna, Austria |
| Ambroin | PF | Ver. Isolatorenwerke A.G. Vienna Austria |
| Amerith | CN | Celluloid Corp. Newark NJ USA |
| Ameroid | CS | American Plastics Corp. New York, USA |
| Amiantine | Copal Plastic | Societe Roux, Paris, France |
| Amzylolithe | CA | Societe Lyonn. de Celluloide, Lyon, France |
| Ardenite | PF | F G Stokes, Ltd. Altrincham, England |
| Argolit | CS | Argo Chem. u. Nahrungsmittel Fabrik., Prerov, Czechoslovakia |
| Askol | PF | Anglo-Scottish Chem. Co. |
| Athrombit | CN | F & M Lautenschlaeger, Munich, Germany |
| Atlas | PF | H Clarke & Co. Manchester, England |
| Atlastik | CN | Atlas Ago Chem. Fab. A.G. Leipzig, Germany |
| Avecolite | PF | Willmott, Sons & Phillips Ltd. England |
| Axolith | CS | Societe l'Oyonnaxienne, Oyonnax, France |

Trade Names B

| Trade Name | Material | Manufacturer |
| --- | --- | --- |
| Bakelaque | PF laquer | Attwater & Sons, Preston, England |
| Bakelite | PF | Bakelite Corp, New York, NY |
| Bandalasta | UF | Brookes & Adams, England |
| Baselon |  | C.Basse & Cie, Luedenscheid, Germany |
| BCM Brownie |  | Brownie Wireless Co, London, England |
| Beacon | UF |  |
| Beatl | UF | Beatl Sales Ltd, England |
| Beetle | UF | Beetle Products Co Ltd, England |
| Belplastic |  | Belplastic Ltd, London W11, England |
| Bennetate | CA |  |
| Bernit | CA | Zelluloidwaren Fabrik, Zollikofen,Switzerland |
| Bex |  | British Xylonite Co. Ltd. London, UK |
| Bexite |  | British Xylonite Co. Ltd. London, UK |
| Bexoid | CA | British Xylonite Co. Ltd. London, UK |
| Bicella | Viscose | Kalle & Co. Wiesbaden-Biebrich,Germany |
| Bikakapseln | Viscose | Kalle & Co. Wiesbaden-Biebrich,Germany |
| Bikarton | PF |  |
| Birmite | PF | E.Elliott, Birmingham |
| Bituba | PF |  |
| Bogophane | Viscose packaging | Soc. Anon. Bogophane, Palermo, Italy |
| Bois durci | albumen | Companie Generale d’Electricite, Paris |
| Bonnywave | PF, UF | Reynolds Spring Co., Jackson, Mich. |
| Boschbakelit | PF |  |
| Britmac | PF, CS | CH Parsons Ltd., Birmingham, UK |
| Britsulite | PF | British Insulite Ltd., Rochdale, UK |
| Brolonkapseln | Viscose stoppers | Chem. Fab. Heyden AG, Dresden-Radebeu, Germany |

Trade Names C

| Trade Name | Material | Manufacturer |
| --- | --- | --- |
| Campbellite | PF laminate | Cambell Fibre Co. Stanton, Del.. |
| Camphoid | CN |  |
| Capes Viscose | Viscose packaging | Du Pont Cellophane Co. Delawanna, NJ |
| Carbolite | PF | Soc. Ind. des Matieres Plastiques, France |
| Carboloid | PF | Carboloid Products Corp. New York, NY |
| Carnalithe | CS | Barthelemy |
| Carta | PF imp. paper | Isola-Werke AG, Duren, Germany |
| Cascaphane | CN | Cascaloid Ltd Leicester, UK |
| Caseilithe | CS | Soc. Ind. du Celluloide, Paris, France |
| Casoide | CS |  |
| Casolith | CS | LM Mears & Co. London, UK |
| Cassoid | Cs | Maison Blanpain, Ezy, France |
| Catalin | PF cast | Amerian Catalin Corp. New York, NY |
| Celanese | CA | Celanese Corp. New York, NY |
| Celastic | CN | Celastic Corp. Arlington, NJ |
| Celastoid | CA | British Celanese Ltd. London, k |
| Celescot | CN | Celescot Co. Toledo, Ohio |
| Cellabutol | CN | IG Farbenindustrie Frankfurt, Germany |
| Cellanite | laminate | Micanite & Insulators Co. London, UK |
| Cellastine | CA | British Celanese Ltd. London, UK |
| Cellemit | CA |  |
| Cellesta | CN | Verein fur Chem. Industrie, Frankfurt, Germany |
| Cellglass | Viscose packaging | Chem. Fab. Cellglass, Holland |
| Cellit | CA | Farbenfabriken Fried. Bayer, Leverkusen, Germany |
| Cellomold | CA | FA Hughes Ltd. London, UK |
| Cellon | CA | Deutsche Celluloid Fabrik, Eilenburg, Germany |
| Cellophan | Viscose packaging | IG Farbenindustrie AG, Frankfurt, Germany |
| Cellophane | Viscose packaging | Societe la Cellophane, Paris, France |
| Cellosite | CA packaging | Ettore Rossi, Milan, Italy |
| Celluclaire | CN packaging |  |
| Celluin | CA | Pavel Rie & Sohn, Prague, Czechoslovakia |
| Celluline | CN |  |
| Cellulit | CS | Societe Ind. du Celuloide, Paris, rance |
| Cellulodine | CN |  |
| Celluloid | CN | Celluloid Corp. Newark, NJ |
| Cellulosine | CN | Cadoret & Degraide |
| Cellutite | CA | G Convert & Cie. Paris, France |
| Celluvert | CS | Soc. Ind. du Celluloide, Paris, France |
| Celoron | PF | Continental-Diamond Fibre Co. Bridgeport, Pa |
| Celtid | CN | Rhein. Gummi u. Cell Fabrik, Mannheim, Germany |
| Cervinite | CA | Zelluloidwaren Fabrik, Zollikofen, Switzerland |
| Cetaphane | Viscose packaging | Transparent Paper Ltd. Bury, UK |
| C-E 950 | PF dentures | Coe Labs. Inc. Chigago, Ill |
| C.F.Board | PF laminate | Campbell Fibre Co. Stanton, Del |
| Cinelin | CN or CA | Cinelin Co. Indianapolis, Ind |
| Ciro | CN records | Celluloid Printers Ltd. England |
| Clar-Apel | Viscose packaging | Du Pont Cellophane Inc. New York, NY |
| Clarifoil | CA packaging | British Celanese Ltd. London, UK |
| Claudilithe | CS |  |
| Clemateite | PF |  |
| Clematite | Bituminous |  |
| Clubman | CA | AW Kanis, London, UK |
| Coltrock | PF cold mold | Colt’s Patent Firearms Mfg. Co. Hartford, Conn |
| Coltstone | Cold mold | Colt’s Patent Firearms Mfg. Co. Hartford, Conn |
| Condensite | PF | Bakelite Corp. New York, NY |
| Coralex | PF | Societe Francaise, Vitry, France |
| Cornalithe | CS | de Charraud, Rueil, France |
| Cornit | Horn plastic |  |
| Coronal | UF | Societe l’Ambrolithe, Paris, France |
| Corozite | CS | Soc. Anon. Prodotti Corozite, Gorlago, Italy |
| Crayonne | CA | Crayonne Ltd, Bexley, Kent, UK |
| Cristalux | CA sheet | Cetate Products Corp. Ltd. London, UK |
| Cristalyx | UF | Edgard Israel, France |
| Cristore | CA | Speights Ltd. UK |
| Crystalite | UF | Rohm & Haas, Philadelphia, Pa |
| Crystillin | PF cast | Crystillin Products Corp. Brooklyn, NY |
| Crystur | UF cast | Panplastics Heyden Chem. Co. Garfield, NJ |
| Cumar | Coumarone resin | Barrett Co. New York, NY |
| Curvitas | CA? | AW Kanis, London, England |

Trade Names D

| Trade Name | Material | Manufacturer |
| --- | --- | --- |
| Damarda | PF lacquer | Bakelite Ltd. London, UK |
| Dekorit | PF cast | Dr. F Raschig, Gmbh, Ludwigshafen, Germany |
| Dilecto | PF laminate | Continental-Diamond-Fbre Co. Newark, Del |
| Dioferrit | CN |  |
| Dobsoid | CS | John Dobson Ltd. Milnthorpe, UK |
| Dorcasine | CS | Charles Horner Ltd. UK |
| Dorex | PF | Dorex, Paris, France |
| Dumold | CN | Du Pont Viscoloid Co. Arlington, NJ |
| Dura C | PF |  |
| Duranoid | PF+shellac | Speciality Mfg. Co. Hoosick Falls, NY |
| Durax | PF | Isola-Werke, Duren, Germany |
| Durez | PF | General Plastics Inc. N.Tonawanda, NY |
| Durite | PF | Stokes & Smith Co. Philadelphia, Pa |
| Durium | PF | Durium Products Corp. New York, NY |
| Duroid | PF | Bakelite Co. France |
| Durolit | PF cast | Societe de Duroid, Enghien, France |
| Durophene | PF | Scott Bader & Co. London, UK |
| Duroware | UF | USA |

Trade Names E

| Trade Name | Material | Manufacturer |
| --- | --- | --- |
| Ebonestos |  | Ebonestos Insulators Ltd. London, UK |
| ECA | CS | Bruggemann & Cia. Mexico |
| Ecaille | PF cast | Labs. Indus. d’Asnieres, Paris France |
| Elastolith | PF cast | Herold AG, Hamburg, Germany |
| Elephantide | laminate | Mica & Insulating Supplies Co. UK |
| Elo | PF | Birkby’s Ltd. Liversedge, Yorkshire, UK |
| Emur | CN | Eberhard Mueller, Remscheid Germany |
| Endura | UF |  |
| Eolit | PF | Kunstharzfabrik, Dr. F Pollak, Vienna, Austria |
| Ergolith | CS | McLeod & McLeod, London, UK |
| Erinite | Ester gum | Erinoid Ltd. Stroud, UK |
| Erinofort | CA | Erinoid Ltd. Stroud, UK |
| Erinoid | CS | Erinoid Ltd. Stroud, UK |
| Esbrilith | CS | Rheinischesfarbwerk, Berlin, Germany |
| Esslinger Zellglass | Viscose packaging | Langheck & Co. Esslingen, Germany |
| Estralit | PF |  |

Trade Names F Trade Name; Material; Manufacturer. Fabroil; PF; General Electric Co. Schenectady, NY. Fabrolite; PF; Commercial Utilities Ltd. London, UK. Fantasit; CS; Rhein. Westfal. Sprengstoff AG, Troisdorf, Germany. Faturan; PF cast; Dr. H Traun u. Sohne, Hamburg, Germany. Ferrozel; PF laminate; Deutsche Ferrozell Ges. Augsburgh, Germany. Fiberloid; CN; Fiberloid Corp, Indian Orchard, Mass. Fibestos; CA; Fiberloid Corp, Indian Orchard, Mass. Fimielite; PF. Firmoid; CN, CA; Bluemel Bros. Ltd. Wolston, UK. Flaka Kapseln; CA; Kalle & Co. AG, Wiesbaden-Biebrich, Germany. Foord’s Casein Plastic; CS+coconut shell. Formalite; PF; Bakelite Ltd. Greet, UK. Formica; PF laminate; Formica Insulation Co. Cincinnati, Ohio. Formite; Pf cast; Bakelite Ltd, Greet, UK.

Trade Names G

| Trade Name | Material | Manufacturer |
| --- | --- | --- |
| Galakerite | CS | Soc. Ital. Galakerite, Milan, Italy |
| Galalith | CS | Intern. Galalith Ges. Harburg, Germany |
| Galatix | CS | Lumos & Co. London, UK |
| Galliperle | CS | Cie. Generale d’Electricite, Paris, France |
| Gaudafil | Viscose packaging |  |
| Gesundheites-Pass | CN | Braun & Co. Berlin, Germany |
| Glider | CA | AW Kanis, London, UK |
| Globerite | CS | Soc. Indus. Globerite, Milan, Italy |
| Glorit | CS | Schiel a Spol. Sternberg, Czeschoslovakia |
| Gummite | Bitumenous | Mfr. d’Isolants et Objets Moules, France |
| Gummon | PF cold moulded | Rhein. Westfal. Sprengstoff AG, Troisdorf, Germany |

Trade Names H

| Trade Name | Material | Manufacturer |
| --- | --- | --- |
| Haefelyte | CS, PF | Emil Haefely & Cie. Basel, Switzerland |
| Hagolit | CA | Gebr. Eckert, Nurnberg, Germany |
| Hai-Ho | CN | Hainich-Holz, Gmbh, Langensalza, Germany |
| Haimanite | Albumen based |  |
| Halex |  | British Xylonite Co. London |
| Halolume | CA | British Elect. Installations Co. London, UK |
| Hares | PF | Roemmler AG, Spremberg, Germany |
| Haresit | PF | Roemmler AG, Spremberg, Germany |
| Harex | PF laminate | Roemmler AG, Spremberg, Germany |
| Harlequin | UF | England |
| Hastra | CS | Hastra Kunstharz Presswerk, Vienna, Austria |
| Haveg | PF | Saeureschutz Ges., Berlin, Germany |
| Hecolite | CN dentures | Heko-Werke, Berlin, Germany |
| Hekolith | CN | Heko-Werke, Berlin, Germany |
| Heliosit | PF | Kontackt-Rommler AG, Frankfurt, Germany |
| Heliozell | Viscose packaging | Feldmuhle Papier u. Zellstoffwerke, Stettin, Germany |
| Herolith | PF | Herold AG, Hamburg, Germany |
| Hornit | CS | Gottfried Probst, Nurnberg, Germany |
| Hyalin | CN |  |
| Hycoloid | CN, CA | Hygienis Tube & Container Co. USA |
| Hyli | CN | Hygienische Ind. Ostertag, Ludwigsberg, Germany |

Trade Names I

| Trade Name | Material | Manufacturer |
| --- | --- | --- |
| Iberolithe | PF | Soc. L’Orolithe, Rueil, France |
| Idelite | PF | Bakelite Ltd., London, UK |
| Idytol | PF |  |
| Inda | CS | Amer. Machine & Foundry Co., Brooklyn, NY |
| Indestructo | CN/glass | Indestructo Glass Corp., Farmingdale, NY |
| Indurite | PF | Indurite Sales Ltd., London, UK |
| Infuselax | UF lacquer | Beetle Products Co., London, UK |
| Insuloid | CA packaging | Harold Levey, New Orleans, USA |
| Isogalithe | CS | Garraud, Tailleburg, France |
| Isolid | PF | Soc. Francaise, Vitry, France |
| Isolierstahl | PF |  |
| Isolit | PF laminate | Soc. Francaise, Lyon, France |
| Isolithe | PF | Soc. Beguin, Paris, France |
| Isoloid | CA | Charles Martn, Levallois, France |
| Isophan | EC packaging | Cellonwerke, Charlottenburg, Germany |
| Ivaleur | CN | Celluloid Corp., Newark, NJ |
| Ivoit | PF | Kunstharzfabrik Dr. F Pollak, Vienna, Austria |
| Ivorax | PF | Herold AG, Hamburg, Germany |
| Ivoride | CN | Daniel Spill & Co., London, UK |
| Ivory Cross | CA | AW Kanis, London, UK |
| Ivrit | PF | Etabliss. Kuhlmann, Paris, France |
| Ivrite | PF | Soc. anon. Ivra, Torino, Italy |
| Ivryne | CS | Etabliss. Feuillant |
| Ixolain | PF dentures |  |

Trade Names J

| Trade Name | Material | Manufacturer |
| --- | --- | --- |
| Jarax | PF laminate | Jaroslaw’s Glimmer-Waren Fab. Berlin, Germany |
| Joanite | PF cast | Joanite Co. Brooklyn, NY |
| Juvelith | PF cast | Kunstharzfabrik, Dr. Pollak, Vienna, Austria |

Trade Names K

| Trade Name | Material | Manufacturer |
| --- | --- | --- |
| Karbolite | PF |  |
| Karolith | CS | American Plastics Corp. New York, NY |
| Kasinoid | CS | AW Kanis, London, UK |
| Kelacoma | PF. UF | Kelacome Ltd., Welwyn Garden City, UK |
| Kellite | PF | Kellogg Switchboard & Supply Co., Chicago, Ill |
| Keralon | CS |  |
| Kerit | CS | Internat. Galalith Ges., Harburg, Germany |
| Keronyx | CS | Aberdeen Combworks Co. Ltd, Aberdeen, UK |
| Kinonglas | CN/glass | N Kinon, Aachen, Germany |
| Kodaloid | CN film | Eastman Kodak Co., Rochester, NY |
| Kodapak | CA | Eastman Kodak Co., Rochester, NY |
| Kopan | PF | Kunstharzfabrik, Dr Pollak, Vienna, Austria |
| Koraton | PF | Wedig & Reuss, Eilenburg, Germany |
| Kyloid | CS | Kyloid Co., Muskegon, Mich. |

Trade Names L

| Trade Name | Material | Manufacturer |
| --- | --- | --- |
| Lacanite | PF | American Record Corp., Scranton, Pa. |
| Laccain | PF | Louis Blumer, Zwickau, Germany |
| Lacrinoid | CS | Lacrinoid Products Ltd., London, UK |
| Lactilith | CS | Charles C Fitzroy, London, UK |
| Lactite | CS |  |
| Lactitis | CS metallic |  |
| Lactoid | CS | British Xylonite Co., UK |
| Lactoite | CS, CN | France |
| Lactolithe | CS | Glogau & Cie., Vitry, France |
| Lactonite | CS | British Lactonie Co., London, UK |
| Lactophane | CS packaging | Poyser Advert. Agency, London, UK |
| Laetelite | CS |  |
| Laminol | PF laminate | Ellison Insulations Ltd., Birmingham, UK |
| Lennite | PF dentures | Ohio Chem. & Mfg. Co., Cleveland, Ohio |
| Leukorit | PF | Dr. F Raschig Gmbh, Ludwigshafen, Germany |
| Linga-Longa | UF | Beatl Sales Co. London, UK |
| Lithene | CA | Plastic Moulding Co. Ltd., London, UK |
| Lonarit | CA | Lonarit Ges., Berlin, Germany |
| Lor-Wal-Lith | PF | Chemie. u. Technik, JMS, Gmbh, Hamburg, Germany |
| Lucent Reel | CN scrap | Rex Campbell & Co., UK |
| Lucienit | PF | Lucien Eilrtsen |
| Lucite | CN, PMMA | Du Pont Viscoloid Co. Arlington, NJ |
| Lugdomite | CA | Societe Lyonnaise de Celluloid, Lyon, France |
| Lumarith | CA | Celluloid Corp. Newark, NJ |
| Lupinite | CS |  |
| Luxalin | CN | Du Pont Viscoloid Co. Arlington, NJ |
| Luxalith | CS | Societe l’Oyonnaxienne, Oyonnax, France |
| Luxan | UF | Luxite Inc. Boston, Mass. |
| Luxite | UF | Luxite Inc. Boston, Mass. |
| Luxolith | CS | Societe l’Oyonnaxienne, Oyonnax, France |

Trade Names M

| Trade Name | Material | Manufacturer |  |
| --- | --- | --- | --- |
| Macoid | CN lacquer | Crawford MacGregor & Canby, Dayton, Ohio |  |
| Magranit | PF laminate | Australia |  |
| Makalot | PF | Makalot Corp., Boston, Mass. |  |
| Maleaze | PF |  |  |
| Marblene | CA sheet | Waite & Son Ltd., London, UK |  |
| Marblette | PF | Marblette Corp., Long Island, NY |  |
| Marbloid | CA sheet | Speights Ltd., London, UK |  |
| Marbolith | PF | Herold AG, Hamburg, Germany |  |
| Margolit | Cold moulded | Ver. Isolaterenwerke AG |  |
| Masa | PF | Masa Gmbh, Berlin, Germany |  |
| Mastolite | PF | Symentis Pdts. Ltd., Eccles, UK |  |
| Masuron | CA | John W Masury & Sons, Brooklyn, NY |  |
| MEC | CA | Minerva Engineering Co., London, UK |  |
| Megohmax | PF | John Moores & Co., Lancashire, UK |  |
| Meghomior | PF | John Moores & Co., Lancashire, UK |  |
| Meghomit | PF | John Moores & Co., Lancashire, UK |  |
| Mergalthe | CS | de Charraud, Rueil, France |  |
| Metakaline | PF |  |  |
| Metduro | PF | Metduro Ltd., London, UK |  |
| Micafolium | PF |  |  |
| Micarta | PF laminate | Westinghouse Elect. & Mfg. Co., Pittsburg, Pa. |  |
| Micolite | PF | Paul Edgard Basset, Paris, France |  |
| M.L. | UF | Beatl Sales Co. London UK |  |
| Moldarta | PF UF | Westing. Elect, & Mfg. Co., Pittsburg, Pa. |  |
| Moldite | CA | American Cellulose & Chem. Mfg. Co., New York, NY |  |
| Monit | Viscose |  |  |
| Moskalit | CS | Moscow State Chem. Trust, Moscow, USSR |  |
| Moldensite | PF | Damard Lacquer Co., Greet, UK |  |
| Mouldrite | PF | Croydon Mouldite Ltd., Croydon, UK |  |
| Trade Names N Trade Name; Material; Manufacturer. Nacara; CN; Fiberloid Corp., Indian Orchard, Mass.. Nacrolaque; CA sheet; Jos. H Meyer Bros., Brooklyn, NY. Nalo; Viscose film; Kalle & Co. Weisbaden –Biebrich, Germany. Neolith; CS; Deutsche Kunsthorn Ges.. Neophan; CA packaging; Cellonwerke, Charlottenburg, Germany. Neoresit; PF; Aug. Nowack AG, Berlin, Germany. Nestorite; PF; James Ferguson & Sons Ltd., Merton Abbey, London, UK. Neutex; CA; Sicherheitsglas Neutex, Aachen Germany. Newtex; CA safey glass; England. Niloid; CN; H Bossi,. Nixonoid; CN; Nixon Nitration Works, Nixon, NJ. Nobeline; PF; Sicoloid Ltd., London, UK. Noveltic; CN; KF Mayer, London, UK. Novite; PF; ICI, London, UK. Novolak; PF; Bakelite Corp., New York, NY. Novolithe; CA; Soc. Bellignite, Bellignat, France. Nymphrap Extra; CA packaging; Sylvania Industrial Corp., Fredercksburg, Va.. |

Trade Names O

| Trade Name | Material | Manufacturer |
| --- | --- | --- |
| Omegite | PF | Brit. Dyestuffs Corp. Ltd., Manchester, UK |
| Opal | PF | Kunstharzfabrik, Fr. Pollak, Vienna, Austria |
| Orlak | PF | Chance Bros. & Co., West Smethwick, UK |
| Ornalith | PF | Herold AG, Hamburg, Germany |
| Orolithe | CA | Soc. D’Orolith, Rueil, France |
| Orthospan | CA | Medical Supply Assoc. Ltd., London, Uk |
| Oxygalalith | CS | France |
| Oyocetil | CA | Soc. L’Oyonnaxienne, Oyonnax, France |
| Oyogalithe | CS | Soc. L’Oyonnaxienne, Oyonnax, France |
| Oyonnithe | Cs | Soc. Petit-Collin-Oyonnithe, Paris, France |

Trade Names P

| Trade Name | Material | Manufacturer |
| --- | --- | --- |
| Panelyte | PF laminate | Panelite Co., Boston, Mass |
| Pantolit | PF cast | Augsburger Kunstharz-Fabrik, Augsburg, Germany |
| Parfait | CN dentures | Parisien Chem. Co., Toledo, Ohio |
| Paxolin | PF laminate | Micanite & Insulators Co., London, Uk |
| Pearlite | CA sheet | Speights Ltd., London, UK |
| Pearloid | CN sheet | Jos. H Meyer Bros., Brooklyn, NY |
| Peralit | PF |  |
| Permaloid | CN | Celluloid Printers Ltd., London, UK |
| Permanite | CN | Parker Pen Co., Jamesville, Wis. |
| Pertinax | PF laminate | Meirowsky & Co., Porz am Rhein, Germany |
| Phenoid | PF laminate | Mica Mfg. Co. Ltd., England |
| Phenolic | PF | American Record Corp., Scranton, Pa. |
| Phenolite | PF laminate | National Vulcanized Fiber Co., Wilmigton, Del. |
| Philite | UF, PF | NV Phillips Gloeilampenfab, Eindhoven, Holland |
| Picaroid | CN sheet | Picaroid Process Ltd., London, UK |
| Plaskon | UF | Toledo Synthetic Products Inc., Toledo, Ohio |
| Plass | UF | Pollopas Ltd., Nottingham, UK |
| Plastacele | CA | Du Pont Viscoloid Co., Arlington, NJ |
| Plastilume | CA | WV Hutchinson, London, UK |
| Plastin | CA | Soc. Des Matieres Plastiques, Paris, France |
| Plastine | CA | Soc. Nobel Francaise, Paris, France |
| Plastine | CA | Sicaloid Ltd., London, UK |
| Plastopal | UF | Pollopas Ltd., London, UK |
| Plastose | PF | Afcom Ltd., London, UK |
| Pluviusim | UF | Kunstharzfabrik, Dr Pollak, Vienna, Austria |
| Plyafix | CS | Jos. Nathan & Co. Ltd., London, UK |
| Plynalith | CS, CA | Isaac Frenkel, Paris, France |
| Pollopas | UF | Kunstharzfabrik, Dr Pollak, Vienna, Austria |
| Pollopas | UF | Pollopas Ltd., London, UK |
| Pollopas | UF | Venditor Gmbh, Berlin, Germany |
| Pollopas-Platten | UF laminate | Venditor Gmbh, Berlin, Germany |
| Porcellanite | CS | Soc. De Charraud, Rueil, France |
| Press Mass | CA | Amer. Brit. Chem. Supplies Inc, New York, NY |
| Pressmikanit | PF |  |
| Presszell | PF |  |
| Primalithe | CS | Cie. de Procedes Plinatus, Paris, France |
| Priscal | UF | Soc. anon. des Matieres Plasiques, Paris, France |
| Progilite | PF | Soc. resins & Vernis Artificiels, Paris, France |
| Protectoid | CA packaging | Celluloid Corp., Newark, NJ |
| Proteolite | CS | Ind. Ital. della Proteolite, Milan, Italy |
| Prystal | UF | Soc. ind. des Matieres Plast., Paris France |
| Prystal | UF | Sicaloid Ltd., London, UK |
| Pyradiolin | CN sheet | Du Pont Viscoloid Co., Arlington, NJ |
| Pryaheel | CN heel cover | Du Pont Viscoloid Co., Arlington, NJ |
| Pyralin | CN | Du Pont Viscoloid Co., Arlington, NJ |
| Pyralin | CN | Canadian Industries Ltd., Montreal, Canada |

Trade Names R

| Trade Name | Material | Manufacturer |
| --- | --- | --- |
| Radite | CN | Sheaffer Pen Co., Fort Madison, Iowa |
| Redmanol | PF | Bakelite Corp., New York, NY |
| Reliance | CN, CA | Reliance Nameplates Ltd., Twickenham, UK |
| Repetit | PF |  |
| Resan | PF | Bakelite Corp., New York, NY |
| Resanit | PF | Kunstharzfabrik Resan, Mosbierbaum, Germany |
| Resinit | PF | Knoll & Co., Ludwigshafen, Germany |
| Resinol | PF | Dr. F Raschig Gmbh, Ludwigshafen, Germany |
| Resinox | PF | Resinox Corp., New York, NY |
| Resin Superba | PF |  |
| Resin Superbo | PF |  |
| Resistan | PF | Kontakt-Rowmmler AG, Frankfurt, Germany |
| Resopal | UF | Rommler AG, Spremberg, Germany |
| Resovin | VInyl denture | SS White Dental Mfg. Co. |
| Rexalith | CS | Soc. la Rexalith, Paris, France |
| Rezelite | PF | Cussons Sons & Co., Manchester, UK |
| Rhodialine | CA packaging | Soc. des Usines Chim. Rhone-Poulenc, Paris, France |
| Rhodialine | CA packaging | May & Baker Ltd., London, UK |
| Rhodoid | CA | Soc. des Usines Chim. Rhone-Poulenc, Paris, France |
| Rhodoid | CA | May & Baker Ltd., London, UK |
| Rhodophane | CA packaging |  |
| Richelain | UF | Richardson Co., Melrose Park, Ill. |
| RJR | CS moulded | Afcom Ltd., London, UK |
| Roanoid | UF | Roanoid Ltd., Glasgow, Scotland |
| Rockite | PF | Rockhard Resins Ltd., London, UK |
| Rockshell | PF | Rockhard Resins Ltd., London, UK |
| Ronilac | UF | Societe La Ronite, Seine, France |
| Ronisol | PF |  |
| Ronite | CA |  |
| Runerit | PF laminate | Electro-Isolier-Industrie, Wahn, Germany |

Trade Names S

| Trade Name | Material | Manufacturer |
| --- | --- | --- |
| Samson-Celluloid | CN film | Celluloid Corp., Newark, NJ |
| Satolite | CS | Sankyo Kabushiki Kaisha, Tokyo, Japan |
| Schellan | UF | Kunstharzfabrik Dr Pollak, Vienna, Austria |
| Schellit | PF | Kunstharzfabrik Dr Pollak, Vienna, Austria |
| Securite | CA | Cie. Petit-Collin-Oyonnithe, Paris, France |
| Seracelle | Viscose film | Courthaulds Ltd., London, UK |
| Setabonite | Resin/rubber | Mfr.d’Isolants et Objets Moules, France |
| Setacegeite | PF | Mfr.d’Isolants et Objets Moules, France |
| Sicalite | CS | Soc. Nobel Francaise, Paris, France Sicaloid Ltd., London, UK |
| Sicoid | CA | Soc. Nobel Francaise, Paris, France Sicaloid Ltd., London, UK |
| Sidac | Viscose film | Sylvania Indust. Corp., Fredericksburg, Va. |
| Sidac | Viscose film | Soc. Ind. de la Cellulose, Ghent, Belgium |
| Sigaleos | PF |  |
| Similex | PF | Labs. Indust. d’Asnieres, Paris, France |
| Similit | PF | Labs. Indust. d’Asnieres, Paris, France |
| Solith | PF | Rejal a Spol., Prague, Csechoslovakia |
| Souvelo | UF | Souvenir Mfg. Co., Birmingham, UK |
| Spauldite | PF laminate | Spalding Fiber Co., N. Rochester, NH |
| Splintex | CA | Splinterless Glass Co. Ltd., Teddington, UK |
| Starkware | UF | USA |
| Sterilin | CA surgical | Germany |
| Streetly | UF | Streetly Mfg. Co. Ltd., London, UK |
| Superisolite | PF |  |
| Sylphrap | CA | Sylvania Indus. Corp., Fredericksburg, Va. |
| Sylvania | Viscose film | Sylvania Indus. Corp., Fredericksburg, Va. |
| Syntholite | PF? | Soc. anon. la Syntholite, Paris, France |
| Syrolit | CS | Syrolit Ltd., Stroud, UK |

Trade Names T

| Trade Name | Material | Manufacturer |
| --- | --- | --- |
| Taumalit | PF | Isopresswerk, Berlin, Germany |
| Telconax | Bitumenous | Teleg. Constr. & Maint. Co., London, UK |
| Telconite | ? | Teleg. Constr. & Maint. Co., London, UK |
| Telenduron | ? | Thomas de la Rue & Co., London, UK |
| Tenalan | PF |  |
| Tenazit | PF | Allgem. Elect. Ges., Berlin, Germany |
| Tenex | CA | Tennessee Eastman Corp., Kingsport, Ten. |
| Textal | Viscose/Aluminium | Auminium Walzwerke AG, Singen, Germany |
| Textolite | PF | Genera Electric Co. Schenectady, NY |
| Text-Tiles | UF tiles | Kelacome Ltd., Welwyn Garden City, UK |
| Thiolite | PF | Soc. Levy, Samuel, et Levy, Joinville, France |
| Tortaloid | CA | Fiberloid Corp., Indian Orchard, Mass. |
| Transparenta | CA film | Transparenta Gmbh, Berlin, Germany |
| Transparit | Viscose packaging | Wolff & Co., Walsrode, Germany |
| Transphan | Cuprammonium film | Bemberg, AG, Wupperthal, Germany |
| Trefoil | PF | Bakelite Ltd., London, UK |
| Trelit | CN | Norway |
| Triacel | CA packaging |  |
| Triolin | CN floor covering | Rheinisch-Westfalische Sprengstoff AG Troisdorf Germany |
| Trolit | CN, CA |  |
| Trolit-Spezial | PF |  |
| Trolitan | PF |  |
| Trolitan H | UF |  |
| Trolitan S | PF |  |
| Trolitax | PF laminate |  |
| Trolitul | Polystyrene |  |
| Trolon | PF |  |
| Trolon-Platten | PF laminate |  |
| Tufnol | PF laminate | Ellison Insulations Ltd., Birmingham, UK |
| Turax | PF |  |
| Turbax | PF laminate | Jaroslow’s Glimmer-Waren Fabrik, Berlin, Germany |
| Turbonit | PF | Jaroslow’s Glimmer-Waren Fabrik, Berlin, Germany |

Trade Names U

| Trade Name | Material | Manufacturer |
| --- | --- | --- |
| Ultraphan | CA packaging | Lonza, Weil am Rhein, Germany |
| Ultrasit | PF | Chem. Fabrik.Ambrasit, Vienna, Austria |
| Unyte | UF | Unyte Corp., New York, NY |
| Uralite | UF | Soc. Resines et Vernis Artificiels, Paris, France |
| Urocristal | UF | Soc. Resines et Vernis Artificiels, Paris, France |
| Utilit | PF | Augsburger Kunstharzfabrik, Augsburg, Germany |

Trade Names V

| Trade Name | Material | Manufacturer |
| --- | --- | --- |
| Veryx | UF | Edgard Israel, France |
| Vigorit | PF | Dr F Raschig, Gmbh, Ludwigshafen, Germany |
| Vinylite | Vinyl resin | Carbide & Carbon Chem. Corp., New York, NY |
| Viralite | CA coated netting | Darlington Fencing Co. Ltd., London, UK |
| Viscacelle | Viscose packaging | Courtaulds Ltd., London, UK |
| Visco | Viscose packaging | Chem. Werke Visco, Aussig, Czechoslovakia |
| Viscocelle | Viscose packaging | Courtalds Ltd., London, UK |
| Viscoloid | CN | Du Pont Viscoloid Co., Leominster, Mass. |
| Visking | Viscose sheeting | Visking Corp., Chicago, Ill. |
| Vitalite | CA | New York Wire Cloth Co., New York, NY |
| Vitreo-Colloid | CA packaging | JM Newton Vitrio-Colloid Ltd., London, UK |
| Vitrex | CA coated netting |  |
| Vitrocelle | Viscose packaging | Dalle Freres et Lecomte, Bousbecque, France |
| Vortex-Burt | PF | Vortex Cup Co., Chicago, Ill. |
| Vydon | Vinyl dentures | LS Smith & Son, Pittsburgh, Pa. |

Trade Names W

| Trade Name | Material | Manufacturer |
| --- | --- | --- |
| Wahnerit | PF laminate | Elect. Isol. Indust., Wahn, Germany |
| Walo-Kapseln | Viscose stoppers | Wolff & Co., Walsrode, germany |
| Wandrite | PF | H Wandrowsky, Berlin, Germany |
| Wenjazit | PF | Kunst-Rohstoff AG, Hamburg, Germany |

Trade Names X

| Trade Name | Material | Manufacturer |
| --- | --- | --- |
| Xetal | CA/glass | England |
| Xilite | PF cast |  |
| Xylonite | CN | British Xylonite Co. Ltd., London, UK |

Trade Names Z

| Trade Name | Material | Manufacturer |
| --- | --- | --- |
| Zellugol | CA |  |
| Zoolite | CS | Soc. Polenghi Lombardo, Codogno, Italy |